1. Cross Hatch Adhesion Test-

| GT0 | No coating removed | ✅ PASS – Excellent adhesion |
| --- | --- | --- |

| GT1 | Small flakes at intersections only | ✅ Acceptable |
| --- | --- | --- |

| GT2–GT5 | Coating removed along edges or in squares |
| --- | --- |

Fail

2. Pencil Hardness Test

| Type of Coating | Acceptable Hardness |
| --- | --- |
| General Powder | ≥ H |
| Architectural Polyester | ≥ 2H |
| Super Durable Polyester | ≥ 3H |

Duracoat Target: 2H minimum.

3. Impact Resistance Test

| Coating Type | Minimum Result |
| --- | --- |

| General Powder | 40 kg·cm |
| --- | --- |

| Architectural Grade | 50 kg·cm |
| --- | --- |

4. Conical Mandrel Bend Test

| Result | Interpretation |
| --- | --- |
| No cracks or detachment | ✅ PASS |
| Slight hairline cracks, no metal exposure | ✅ Acceptable |
| Coating peeled or detached | ❌ Fail |

5. Cupping Test

Pass Criteria

| Coating Type | Minimum Depth (mm) |
| --- | --- |
| Industrial Powder | 6 mm |
| Architectural Grade | 8 mm |

Duracoat Acceptance: ≥ 8 mm, no cracking.

6. Gloss Measurement Test

Pass Criteria

| Finish Type |  |  | Gloss Units (GU) |
| --- | --- | --- | --- |
| Matt |  |  | 10–30 GU (85°) |
| Semi-Gloss |  |  | 31–70 GU (60°) |
| Gloss |  |  | 71–95 GU (60°) |
| 7. Powder Flowability Test |  |  | (In house test 15days) |
| Result | Interpretation |

| 10–25 sec for 50 g | ✅ Good flow |
| --- | --- |

| 26–40 sec | ⚠️ Moderate |
| --- | --- |

| >40 sec or blockage | ❌ Poor (may cause orange peel) |
| --- | --- |

8. Heat chamber calibration test (90 days) –

Summary — Duracoat Acceptance Table

| Test | Standard | Duracoat Pass Value |
| --- | --- | --- |
| Cross Hatch | ISO 2409 | GT0 – GT1 |
| Pencil Hardness | ASTM D3363 | ≥ 2H |
| Impact Resistance | ISO 6272 | No crack @ 50 kg·cm |
| Mandrel Bend | ISO 6860 | No visible cracking |
| Cupping | ISO 1520 | ≥ 8 mm |
| Gloss | ISO 2813 | Within ±5 GU |
| Flowability | ISO 8130-3 | 15–25 sec / 50g |
| Salt Spray | ASTM B117 | ≤ 2 mm edge creep (500 hrs) |

DURACOAT POWDER COATING — QUALITY TEST PROCEDURES & PASS CRITERIA

1️⃣ Cross Hatch Adhesion Test

Standard: ISO 2409 / ASTM D3359
Instrument: Cross Hatch Cutter, Adhesive Tape (3M 600 type), Magnifier

🔹 Purpose

To check how well the powder coating film adheres to the metal substrate.

🔹 Test Procedure

- Use a cross hatch cutter with 1 mm or 2 mm spacing.

- Cut six parallel lines through the coating to the substrate.

- Rotate the panel 90° and make another six cuts to form a grid (like a chessboard).

- Brush off dust gently.

- Apply adhesive tape over the cut area and press firmly.

- Peel off at 45° angle in one quick motion.

- Examine under 10× magnifier.

🔹 Pass Criteria

| Grade (ISO 2409) | Description | Result |
| --- | --- | --- |
| GT0 | No coating removed | ✅ PASS – Excellent adhesion |
| GT1 | Small flakes at intersections only | ✅ Acceptable |
| GT2–GT5 | Coating removed along edges or in squares | ❌ Fail |

Duracoat Acceptance: GT0 or GT1.

2️⃣ Pencil Hardness Test

Standard: ASTM D3363
Instrument: Pencil Hardness Tester, Mitsubishi or Faber Castell Pencils (6B–6H)

🔹 Purpose

To determine surface hardness or scratch resistance of the coating.

🔹 Test Procedure

- Prepare pencil leads (6B = softest, 6H = hardest).

- Place the coated panel flat.

- Hold the pencil at a 45° angle to the surface.

- Push the pencil forward 6–10 mm with steady pressure.

- Start from soft (B) and go harder (H, 2H, etc.) until the film just scratches.

- Record the hardest pencil that does not scratch the coating.

🔹 Pass Criteria

| Type of Coating | Acceptable Hardness |
| --- | --- |
| General Powder | ≥ H |
| Architectural Polyester | ≥ 2H |
| Super Durable Polyester | ≥ 3H |

Duracoat Target: 2H minimum.

3️⃣ Impact Resistance Test

Standard: ISO 6272 / ASTM D2794
Instrument: Impact Tester (½ kg weight, ½ inch punch)

🔹 Purpose

To evaluate flexibility and adhesion under sudden impact.

🔹 Test Procedure

- Place the coated panel on the tester, coating facing down.

- Drop a ½ kg weight from a known height (e.g., 50 cm).

- Inspect the reverse side for cracks, flaking, or delamination.

- Perform both direct and reverse impact (impact on coated and uncoated sides).

🔹 Pass Criteria

| Coating Type | Minimum Result |
| --- | --- |
| General Powder | 40 kg·cm |
| Architectural Grade | 50 kg·cm |

Duracoat Acceptance: No cracks or detachment at 50 kg·cm.

4️⃣ Conical Mandrel Bend Test

Standard: ISO 6860 / ASTM D522
Instrument: Conical Mandrel Bend Tester

🔹 Purpose

To assess flexibility and adhesion during bending or forming.

🔹 Test Procedure

- Fix the coated panel in the tester.

- Bend the panel gradually around the mandrel (from 3 mm to 38 mm diameter).

- Observe the bent area for cracks, peeling, or loss of adhesion.

🔹 Pass Criteria

| Result | Interpretation |
| --- | --- |
| No cracks or detachment | ✅ PASS |
| Slight hairline cracks, no metal exposure | ✅ Acceptable |
| Coating peeled or detached | ❌ Fail |

Duracoat Target: No visible cracking across the full bend.

5️⃣ Cupping Test

Standard: ISO 1520
Instrument: Erichsen Cupping Tester

🔹 Purpose

To determine the ductility of the coating under deformation (stretching).

🔹 Test Procedure

- Clamp coated panel on tester.

- Push a steel ball (20 mm dia.) slowly upward until coating cracks.

- Record the depth of indentation (mm) where the first crack appears.

🔹 Pass Criteria

| Coating Type | Minimum Depth (mm) |
| --- | --- |
| Industrial Powder | 6 mm |
| Architectural Grade | 8 mm |

Duracoat Acceptance: ≥ 8 mm, no cracking.

6️⃣ Gloss Measurement Test

Standard: ISO 2813 / ASTM D523
Instrument: Gloss Meter (20°, 60°, 85° angles)

🔹 Purpose

To measure surface reflectivity (shininess) of the coating.

🔹 Test Procedure

- Calibrate gloss meter using standard calibration tile.

- Place instrument flat on the coated surface.

- Take readings at 60° angle (standard), or at 20° for high-gloss, 85° for matte.

- Record average of 3–5 readings.

🔹 Pass Criteria

| Finish Type | Gloss Units (GU) |
| --- | --- |
| Matt | 10–30 GU (85°) |
| Semi-Gloss | 31–70 GU (60°) |
| Gloss | 71–95 GU (60°) |

Duracoat Acceptance: Must be within customer-specified gloss range (±5 GU tolerance).

7️⃣ Powder Flowability Test

Standard: ASTM D1895 / ISO 8130-3
Instrument: Powder Flow Tester (Hall Flow Meter)

🔹 Purpose

To test powder flow characteristics – important for smooth coating finish.

🔹 Test Procedure

- Weigh 50 g of powder.

- Allow it to flow through a standard funnel orifice (2.5 mm or 4 mm).

- Record the time (seconds) it takes for all powder to flow out.

- If powder does not flow freely, repeat after sieving or drying.

🔹 Pass Criteria

| Result | Interpretation |
| --- | --- |
| 10–25 sec for 50 g | ✅ Good flow |
| 26–40 sec | ⚠️ Moderate |
| >40 sec or blockage | ❌ Poor (may cause orange peel) |

Duracoat Target: 15–25 sec / 50 g — indicates good electrostatic application property.

8️⃣ Salt Spray (Fog) Test

Standard: ASTM B117 / ISO 9227
Instrument: Salt Spray Test Chamber

🔹 Purpose

To assess corrosion resistance of coated samples.

🔹 Test Procedure

- Prepare 3 test panels with coated edges.

- Scratch an “X” mark through coating to bare metal.

- Place in salt spray chamber (5% NaCl, pH 6.5–7.2, 35°C).

- Inspect after 500 hours exposure.

- Examine for blistering, rust, and edge creep.

🔹 Pass Criteria

| Duration (hrs) | Condition | Pass Limit |
| --- | --- | --- |
| 250 hrs | No blisters, rust, or creepage >1 mm | ✅ PASS |
| 500 hrs | No blisters, rust, or creepage >2 mm | ✅ PASS (Architectural) |
| 1000 hrs | Very high-durability (Super Durable Grade) | ✅ PASS |

Duracoat Target: No blistering / ≤2 mm edge creep after 500 hrs.

✅ Summary — Duracoat Acceptance Table

| Test | Standard | Duracoat Pass Value |
| --- | --- | --- |
| Cross Hatch | ISO 2409 | GT0 – GT1 |
| Pencil Hardness | ASTM D3363 | ≥ 2H |
| Impact Resistance | ISO 6272 | No crack @ 50 kg·cm |
| Mandrel Bend | ISO 6860 | No visible cracking |
| Cupping | ISO 1520 | ≥ 8 mm |
| Gloss | ISO 2813 | Within ±5 GU |
| Flowability | ISO 8130-3 | 15–25 sec / 50g |
| Salt Spray | ASTM B117 | ≤ 2 mm edge creep (500 hrs) |